## Slide 1: Atomistic thermodynamics
including pressure and temperature

## Slide 2: DFT – 0K, 0 Pa
DFT calculations provide the energy at 0K, in vacuum
Most properties are affected by pressure and temperature
Atomistic thermodynamics provides a mechanism to connect DFT to pressure and temperature
We need a way to connect the relevant energies to thermodynamic reservoirs.
In other words, if you put an adsorbate on a surface you gain some energy, but that energy is offset by the energy it took to take the adsorbate from the reservoir
Notes: http://ftp.rta.nato.int/public//PubFullText/RTO/EN/RTO-EN-AVT-142///EN-AVT-142-02.pdf

## Slide 3: Reformulating the energy equations
We have typically only examined differences in DFT total energies
  These are like internal energies (U)
  They have no pV (enthalpy) terms or TS (entropy) terms
The general approach is to formulate everything in terms of Gibbs free energies and simplify where appropriate

## Slide 4: Gibbs free energy formulation
The total Gibbs free energy of this system is
Let’s consider the case where the surface is uniform. Then we can express the surface energy as:
And note that this is defined by a finite part of the system, namely the surface region. As the system grows large, the contributions from the infinite portion of the system eventually cancel.

## Slide 5: Chemical potential formalism
We are interested in the cost to take a molecule from a thermodynamic reservoir
  This is the chemical potential
The chemical potential defines the energy required to add or take something from a thermodynamic reservoir
It is temperature and pressure dependent

## Slide 6: Surface energy in chemical potential terms

## Slide 7: Alternative, equivalent formulation focus on adsorption energy
This shows the adsorption energy can be thought of in terms of differences in surface energy
exothermic adsorption lowers the surface energy
Adsorption energies depend on T,p

## Slide 8: From Gibbs to DFT
The Gibbs free energy formulation is exact, but we do not calculate G directly
We need a set of systematic approximations to get from G to DFT for each term in the equation

## Slide 9: Gas phase chemical potentials
Major assumption: Ideal gas law is adequate
The partition function (Q) contains contributions from translation, rotation, vibrations, electronic and nuclear contributions
All of these can be calculated using DFT, but a simpler approach is often used

## Slide 10: Janaf thermodynamic tables
This is the equation relating the DFT energy of O2 to a non-zero pressure and temperature
Can be applied to other gas-phase adsorbates
Notes: 1. K. Reuter and M. Scheffler, Composition, structure, and stability of RuO2(110) as a function of oxygen pressure. Physical Review B, 2002. 65(3): p. 035406. (http://dx.doi.org/10.1103/PhysRevB.65.035406 )

## Slide 11: Solid phase Gibbs energies
The key to what follows is that G is not the relevant energy, but G
So we focus on what terms dominate G
Dimensional analysis leads to: [pV/A] = atm Å3/Å2 ~ 10-3 meV/Å2
We neglect the pV dependence on G

## Slide 12: Vibrational contributions
We often will neglect Fvib
It tends to be small except at very high T
ΔFvib,ad always stays within ≈ ±5 meV/ Å2 for this system
You need to evaluate this for each system
It requires an estimation of phonon DOS of the two systems (clean and covered)

## Slide 13: Configurational free energy
Requires a statistical mechanical treatment to be rigorous
Simple estimate:
With a typical area per surface site of A ~ 10 Å2 for transition metal surfaces, we correspondingly deduce that the configurational entropy contribution to the Gibbs free energy is less than 3 meV/ Å2 for any T < 1000 K [15].
And hence we neglect that too, for pure systems.

## Slide 14: What is left?
G E for bulk solids
Care must be taken for other systems where
  defects or configurational disorder is high
  Large changes in vibrational characteristics of the two states
  Soft materials where pV is important

## Slide 15: Case study in simple adsorption
This is the definition for an average binding energy
Note it has the opposite sign convention from typical thermodynamics
This leads to the following definition for the adsorption energy
Forming a surface with No oxygen atoms gains Eb per atom
At a cost of No atoms from the gas reservoir
The middle term accounts for cases where there are more metal atoms in the oxidized surface than in the clean surface

## Slide 16: What are the questions?
Given a pO2 and T, which surface structure is most stable?
  The one with the lowest surface energy
The surface energy depends on the number of oxygen atoms and the chemical potential

## Slide 17: limiting cases
clean surfaces have a constant surface energy
  neglecting temperature dependent vibrational and configurational free energy
In the limit of o = -, all surfaces are clean
G becomes very positive due to entropy

## Slide 18: Transition from clean to adsorbate covered
when ΔμO = –Eb the adsorbate covered surface is as stable as the clean surface
For more positive ΔμO the adsorbate covered surface is more stable than the clean surface

## Slide 19: Upper bound on number of oxygens
The highest number of oxygen atoms a surface can accommodate is in the bulk oxide phase
  in a thick oxide layer on top of the metal No  and the slope of the o dependence approaches 
This occurs at a o where the bulk oxide is more favorable than metal and gas phase oxygen

## Slide 20: Summarizing the oxidation of Pd

## Slide 21: Gold oxidation example
Different facets change surface energy at different rates
Notes: 1. H.Q. Shi and C. Stampfl, Shape and surface structure of gold nanoparticles under oxidizing conditions. Physical Review B, 2008. 77(9): p. 094127. (http://dx.doi.org/10.1103/Physrevb.77.094127)

## Slide 22: Effect on particle shape

## Slide 23: More complicated example – Sulfur poisoning and multiple adsorbates
Given multiple gas species, how do we estimate surface coverages?
Consider Cu surfaces with gas phase H2, H2S, CO, CO2, H2O

## Slide 24: Chemical potential determined by equilibrium reactions

## Slide 25: Defining chemical potentials

## Slide 26: Multicomponent surface energies

## Slide 27: Adsorption of S on Cu surfaces
H2SS* + H2
Cu(111)
Cu(110)
Cu(100)

## Slide 28: CO adsorption
COCO*

## Slide 29: Effect of surface energy changes on particle shape
Use the Wulff construction to estimate particle shapes
Shapes change because the relative surface energies of each facet change at different rates with sulfur chemical potential
Notes: http://cad4.cpac.washington.edu/winxmorphhome/winxmorph.htm

## Slide 30: Experimental evidence of environment induced shape cahnge
http://lib.semi.ac.cn:8080/tsh/dzzy/wsqk/science/vol295/295-2053.pdf
Notes: http://lib.semi.ac.cn:8080/tsh/dzzy/wsqk/science/vol295/295-2053.pdf

## Slide 31: Reversible shape change in reducing/oxidizing environments

## Slide 32: oxygen adsorption on Cu surfaces
H2OO* + H2